The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep21sc-1.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Rigid, Abrasion Resistant Two Component Epoxy for Bonding, Coating and Sealing Applications

Engineered with a silicon carbide filler material, Master Bond EP21SC-1 delivers abrasion resistance for an array of chemical and mechanical processing applications. This epoxy has a smooth paste consistency and a non-critical one to one mix ratio by weight or volume. As a two part system, it cures readily at room temperature or more quickly at elevated temperatures.

With a Shore D hardness exceeding 95, EP21SC-1 is a rigid compound that adheres well to treated metals, ceramics and many plastics. Its physical strength profile includes a tensile strength greater than 6,000 psi and a compressive strength of over 15,000 psi at room temperature. Since the system is 100% reactive and does not contain any solvents or diluents, it has minimal shrinkage upon cure. Additionally, EP21SC-1 is capable of withstanding a range of chemicals such as water, oils, hydraulic fluids, acids and bases. The combination of the aforementioned properties enables this system to be widely employed for maintenance and repair of pumps, chutes, centrifuges, impellers and tanks.

EP21SC-1 is serviceable from -60°F to +250°F. It is a competent electrical insulator and it has a low thermal expansion coefficient. Both Parts A and B are dark gray in color and are available in standard packaging ranging from pint to 5 gallon container kits.

Master Bond Chemical Resistant Adhesives

Master Bond EP21SC-1 features abrasion resistance and convenient handling for bonding, coating and sealing applications. This two component epoxy also resists a variety of chemicals.

Read more about Master Bond’s chemical resistant epoxies at http://www.masterbond.com/properties/chemical-resistance or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep21sc-1

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #